## Slide 1: Droplets form the films

## Slide 2: Importing Data
Step 1
Parameters | values | Notes
Ndroplet | 1~8 | The number of Pt droplet.
L | 170 | The simulation box size.
c | 1 | The space grid size.
dt | 0.01c2 | The time step.
N | L/c | The length of the data matrix.
thickness | 0.011 | The dimensionless thickness of a PtSex monolayer, which governs the consumption rate of Pt droplets during motion..
Rball | 15 | The initial radius of Pt droplets.
Rc | 35 | The critical radius above which Pt droplets solidify hence cease to move.
φ | -1, 1 | The order parameter, whereas -1 represents the bare MoS2 substrate, and 1 represents the PtSex single layer.
λ | 10 | The dimensionless coupling constant

## Slide 3: Running Code
Step 2
Select the required Ndroplet to droplet numbers, click on the “Run” button in MATLAB or Octave. A new figure window will show up. Pt droplets selenized to form PtSex films drive the motion of the droplets, leaving a earthworm-like trail. Once the number of droplets reaches a certain threshold, a complete monolayer film of PtSex can be formed..
Ndroplet=1
Ndroplet=3
Ndroplet=8

## Slide 4: Droplet climbs the film

## Slide 5: Importing Data
Step 1
Parameters | values | Notes
Lx, Ly, Lz | 64 | The X, Y, and Z sizes of the simulation box.
R | 8~12 | The radius of the Pt droplet, while a smaller droplet will stay at step, and larger one will climb the step.
λ | 180 | The coupling constant.
c | 0.5 | The space step size along either X, Y, and Z.
dt | 0.01c2 | The time step.
K | 1 | The droplet’s surface tension in simulation.
r | (x+5) 2+y2+(z-5)2 | Setting droplet at film step initially.
ρ | Sign(R2-r2)/2+0.5 | The phase-field for the density of the liquid. ρ = 1 denotes liquid phase and ρ = 0 denotes the vapor phase.
Note: The introduction of the wetting angle θ is in lines 42 and 43 of the code. We set ρs=0.6323 such that the θ between Pt/PtSex is 67.2°, and ρs=0.5064 (0.6323-0.1259) such that the θ between Pt/MoS2 is 88.9°.

## Slide 6: Running Code
Step 2
Select the required R to droplet sizes, click on the “Run” button in MATLAB or Octave. A new figure window will show up. The smaller droplet will stay at step, and larger one will climb the step.
R=10
R=8